## Slide 1
Picosecond Time-Resolved Studies of Exciton Transport in Conjugated Polymer Nanoparticles
Department of Chemistry
Louis C. Groff II

## Slide 2: Outline
Background
  Conjugated Polymers & Nanoparticles
  Why Study CPNs?
  Excited States in CPs and CPNs
Dye-Doped PFBT CPNs
  Red-shifted Emission
  Complex Fluorescence Lifetime Kinetics
  Modeling to Determine Intrinsic LD
Solvent-Induced Swelling of CPNs
  Fluorescence Quantum Yield/Spectral Shifting
  Picosecond Decay Kinetics
  Fluorescence Anisotropy Decay
  Lattice Model
  Quantum Yield/Mobility Tradeoff
Summary
Acknowledgements

## Slide 3: Conjugated Polymers – Basic Photophysics
Plastic, amorphous organic semiconductors
  Useful for low cost, flexible photovoltaics, LEDs and solar cells
Repurposing CPs to make nanoparticles
  Have many useful optical properties
Dennler, G., Sariciftci, N.S., Proc. IEEE 2005, 93 (8), 1429.
Yim, K., Kim, J. S. et al., Adv. Func. Mater. 2008, 18, 1012.
Scholes, G., Rumbles, G., Nature Mater. 2006, 5, 683.
http://s1.ibtimes.com/sites/www.ibtimes.com/files/styles/v2_article_large/public/2014/01/15/samsungflexibleamoledphone.jpg
Background
Flexible Amorphous OLED Screen Prototype

## Slide 4: Conjugated Polymer Nanoparticles (CPNs)
Optical Properties
  Extended π-conjugated chains
    Structure, Heteroatoms: HOMO/LUMO gap in UV/Vis
    Wide range of colors
  High chromophore number density
    Increased by nanoparticle formation
  Highly fluorescent
  Efficient Förster energy transfer hosts/dopants
    Red-shifting, sensors
    Wavelength tunability
Background

## Slide 5: CP Properties and Structure
Solvent-Induced Swelling
conjugated polymer nanoparticle
conjugated polymer film
conjugated polymer in solution
Properties of conjugated polymers depend critically on nanoscale structure, heterogeneity, inter/intrachain interactions and other nm scale processes
  Energy transfer and charge transfer
CPNs comprised of one or more collapsed chains
  Nanoscale, disordered, multichromophoric system
  Studies of single CPNs provide unique perspective on nanoscale phenomena

## Slide 6: Milestones in CPN Research
Brightest (5-20 nm) nanoparticle probes reported to date
1000x brighter two-photon fluorescence compared to conventional dyes
Effective fluorescent probes for imaging of cancer cells
Novel oxygen sensing NPs
Wu, C. F., Szymanski, C., Cain, Z., and McNeill, J. D. J. Am. Chem. Soc. 2007, 129, 12904-12905.
Wu, C. F., Bull, B., Christensen, K., and McNeill, J. D. Angew. Chem. Int. Ed. 2009, 48, 2741-2745.
Wu, C. F., McNeill, J. D., Chiu, D. T., et. al. J. Am. Chem. Soc. 2010, 132, 15410-15417.
Background
Confocal Imaging of Human Breast Cancer Cells
Two-Photon Brightness Comparisons
Oxygen Sensing CPNs

## Slide 7: Why Study CPNs? – Imaging
Brighter fluorescent probes still needed for imaging applications
  CPNs are the brightest small fluorescent probes reported to date
    30x higher emission intensity compared to Quantum Dots
    High quantum yield, fluorescence cross sections
  Improvements in quantum yield and photostability are still needed
C. Wu, J. McNeill, Chiu, D. et al., J. Am. Chem. Soc. 2008, 132 (43), 15410
Background
CPNs
CdSe
Quantum Dots
Brightness/Volume Ratios of Various Probes

## Slide 8: Why Study CPNs? – Imaging
Red-shifting needed for imaging applications
  overcome background cell autofluorescence
  Improve brightness, photostability
  Have previously accomplished this via doping CPNs with other CPs or dyes
C. Wu, J. McNeill et al., J. Phys. Chem. B 2006, 110 (29), 14148
C. Wu, J. McNeill et al., J. Phys. Chem. C 2008,112 (6), 1772
Red-shifting of fluorescence via polymer blending
Red-shifting of fluorescence via dye doping
Brighter, more photostable particles via doping
Background

## Slide 9: Why Study CPNs? – Imaging
CPNs are non-toxic to cells
  No heavy metals
  Allows for imaging in live cells
Easily functionalized
  Can functionalize or bioconjugate CPNs for use in cellular media
Challenges:
  Cell media are complex
    Background autofluorescence
    Requires bright, red-shifted particles
Wu, C., McNeill, J., Chiu, T. et al., J. Am. Chem. Soc. 2010, 132, 15410
Background

## Slide 10: Why Study CPNs? - Devices
Optimize organic semiconductor devices such as LEDs, solar cells
Conjugated polymer devices made by thin film casting
  Bulk heterojunction film sandwiched between cathode/anode materials
  Photoexcitation of film generates Frenkel excitons
  Exciton transport to nano- microscale polymer interfaces
  Charge transfer to generate electron and hole pair
  Charges travel to cathode/anode materials
Heeger, A. J., Adv. Mater. 2014, 26, 10-28
Günes, S., Neugebauer, H., and Sariciftci, N. S. Chem. Rev. 2007, 107, 1234-1338.
Background

## Slide 11: Why Study CPNs? – Photophysics
Many radiative and non-radiative processes occur in CPNs
  Conventional radiative/non-radiative decay
  Polaron generation/quenching by polarons
  Quenching by defects
  Energy transfer to dopants
Interested in determining the rates of energy transfer in CPNs
Background

## Slide 12: Excited States in Conjugated Polymers & CPNs: Frenkel Excitons
Chromophore
  Result of delocalized pz orbitals
  Individual chromophores are ~2-8 monomer units in length
Molecular/Frenkel Exciton
  Delocalized Excitation
  Interacting transition dipoles between adjacent chromophores (perturbation theory)
Background
Frenkel, J. Phys. Rev. 1931, 37, 1276-1294.
Kasha, M. Rawls, H. R., and Ashraf El-Bayoumi, M. Pure Appl. Chem. 1965, 11, 371-392

## Slide 13: Excited States in Conjugated Polymers & CPNs: Exciton Dimer Model
Simplest Case: Dimer
  Zero-order: two isolated chromophores
  Energies correspond to excitation at respective sites
  Introduce perturbation
    Linear Combinations of Zero-Order States
    Perturbed/Mixed states and energy and DE(0)
  Different States/energy for non-degenerate and degenerate cases
Background
Hamiltonian
Zero-order states/energy
Perturbed/Mixed States
Perturbation
Atkins, P.; Friedman, R. Molecular Quantum Mechanics; Fourth ed.; Oxford University Press: New York, 2005

## Slide 14: Excited States in Conjugated Polymers & CPNs: Exciton Dimer Model
Non-degenerate chromophores
  Weakly mixed states
  Small energy shift
  Incoherent energy transport (FRET)
Degenerate Chromophores
  Evenly mixed states
  Large energy shift
  Coherent energy transport
Background
Atkins, P.; Friedman, R. Molecular Quantum Mechanics; Fourth ed.; Oxford University Press: New York, 2005

## Slide 15: Excited States in Conjugated Polymers & CPNs: Exciton Dimer Model
Non-degenerate chromophores
  Weakly mixed states
  Small energy shift
  Describes incoherent energy transport (FRET)
Degenerate Chromophores
  Evenly mixed states
  Large energy shift
  Describes coherent energy transport
Background
Atkins, P.; Friedman, R. Molecular Quantum Mechanics; Fourth ed.; Oxford University Press: New York, 2005

## Slide 16: Excited States in Conjugated Polymers & CPNs: Light and Dark Exciton States
Transition dipole coupling splits energy levels of chromophores
  T. dipole orientation dictates which state contributes to emission signal
  Related to molecular orientation
  Nonzero transition dipole vector sum  emissive state
Basis of H- and J-aggregate spectral characteristics
Background
Jelley, E. E. Nature (London) 1937, 139, 631-632.
Wurthner, F., Kaiser, T. E., and Saha-Moller, C. R. Angew. Chem. Int. Edit. 2011, 50, 3376-3410.

## Slide 17: Excited States in Conjugated Polymers & CPNs: Exciton Transport
Two types of energy transport
  Coherent transport
    Degenerate Chromophores
    No/low disorder
    Strong coupling
    Low T
  Oscillating excitation across chromophores (fs time scale)
Background
Coherent Energy Transfer Probability
Loudon, R. The Quantum Theory of Light; Third ed.; Oxford University Press, 2000
Collini, E., and Scholes, G. D., Science 2009, 323, 369-373.

## Slide 18: Excited States in Conjugated Polymers & CPNs: Exciton Transport
Two types of energy transport
  Incoherent transport
    Non-degenerate chromophores
    Significant disorder
    Weak coupling
    High (e.g. room) T
  Energy transfer along or between chains, or to dopants (ps time scale)
Background
Incoherent Energy Transfer Probability
Collini, E., and Scholes, G. D., Science 2009, 323, 369-373.
Atkins, P.; Friedman, R. Molecular Quantum Mechanics; Fourth ed.; Oxford University Press: New York, 2005

## Slide 19: Conventional Exciton Diffusion Length Measurement
Exciton Diffusion Length
  Length exciton is transported during exciton lifetime
  Measured using doped or layered film samples, or direct imaging methods (e.g. NSOM)
CPNs exhibit similar photophysics to thin films
Fewer challenges/pitfalls compared to films
  Pinholes in film (direct acceptor excitation)
  Optical penetration depths > length scales of energy transport
  Layer segregation issues
  Quenching by surface plasmons of metal anode/cathode (in electroluminescent samples)
Lunt, R. R., Giebink, N. C., Belak, A. A., Benzinger, J. B., and Forrest, S. R. J. Appl. Phys. 2009, 105, 053711-053717.
McNeill, J. D., O’Connor, D. B., and Barbara, P. F. J. Chem. Phys. 2000, 112, 7811-7821.
Background

## Slide 20: CPN Photophysics
Want a model that can explain the complex photophysics of CPNs
  Exciton Diffusion Energy Transfer Model
Want to understand the underlying rate processes in CPNs as well as the length and time scales of nanoscale events in CPNs
  Aid in optimizing CPNs for imaging applications and photovoltaic/OLED applications
  Utilize a variety of time-resolved techniques to address these issues from multiple angles
Background

## Slide 21: Red-shifted CPNs via Förster Resonance Energy Transfer
PFBT – Host Polymer
Very photostable (~109 photons/CPN emitted before photobleaching)
High quantum yield (0.66 in THF)
Broad emission spectrum
Perylene Red – Nonpolar dye dopant
High quantum yield (0.98 in DCM)
Laser dye – highly photostable
Excellent spectral overlap with PFBT
Red-shifted emission spectrum
Dye-Doped PFBT CPNs
Groff, L. C., Wang, X., McNeill, J. D., J. Phys. Chem. C 2013, 117, 25748.

## Slide 22: Preparing Dye-doped CPNs
Reprecipitation method
  Polymer/dye dissolved in THF
  Dilute solution
  Rapidly mix with water under sonication (30 s)
  Remove THF and filter to remove large aggregates
  Mean particle size ~10 nm
Dye-Doped PFBT CPNs
Groff, L. C., Wang, X., McNeill, J. D., J. Phys. Chem. C 2013, 117, 25748.

## Slide 23: Förster Resonance Energy Transfer
Interacting chromophore transition dipoles
  Related to dimer model
  Yields dependence
Non-radiative energy transfer from donor to acceptor
Donor/acceptor can be identical or different
  Identical: Homotransfer
    Degenerate chromophores
    Thermal disorder causes incoherent transfer
  Different: Heterotransfer
    Transfer to dopants or defects
Lakowicz, J. R., Principles of Fluorescence Spectroscopy. Third ed.; New York, 2006.
Förster, T. Ann. Phys. 1948, 437, 55-75.
Dye-Doped PFBT CPNs
Energy Transfer Rate Constant

## Slide 24: Förster Resonance Energy Transfer
Energy transfer efficiency depends on spectral overlap, distance between donor/acceptor and orientation
  Scales as R-6
  Useful as “molecular ruler”
Förster Radus (R0)
  Distance at which energy transfer efficiency = 50%
  Typically < 10 nm
http://bio.physics.illinois.edu/newTechnique.html
Lakowicz, J. R., Principles of Fluorescence Spectroscopy. Third ed.; New York, 2006.
Stryer, L. Annu. Rev. Biochem. 1978, 47, 819-846.
Dye-Doped PFBT CPNs

## Slide 25: Red-shifted, High Quantum Yield Dye-doped CPNs
Efficient quenching of PFBT emission by perylene red
  86% quenching at 2% perylene red
Quenching obeys Stern-Volmer equation
Perylene red emission red-shifts with increasing doping
Aggregation quenching of acceptor at higher concentrations
  Dynamic Quenching
  Likely due to dye dimers in CPNs (J-aggregates)
Dye-Doped PFBT CPNs
Stern-Volmer Equation
Groff, L. C., Wang, X., McNeill, J. D., J. Phys. Chem. C 2013, 117, 25748.

## Slide 26: Red-shifted, High Quantum Yield Dye-doped CPNs
Successfully red-shifted particle emission
CPN quantum yield not substantially reduced from 0.1% to 1% doping while ET is high
  Photostability may be improved by doping
  Saturated emission rate may also be improved by doping
Dye-Doped PFBT CPNs
Stern-Volmer Equation
Groff, L. C., Wang, X., McNeill, J. D., J. Phys. Chem. C 2013, 117, 25748.

## Slide 27: Fluorescence Quenching and Lifetimes
It is evidenced by fluorescence spectra that perylene red efficiently quenches emission
  Is this quenching static or dynamic?
What are the fluorescence lifetimes of the doped samples?
  Previous work indicates PFBT CPN lifetimes on the picosecond time scale
  Do these samples exhibit complex decay kinetics?
What is the correct physical picture in terms of rate processes?
C. Wu, J. McNeill et al., ACS Nano, 2008, 2, 2415
Dye-Doped PFBT CPNs

## Slide 28: Picosecond Time-Correlated Single-Photon Counting (TCSPC) Spectroscopy
Ultrafast, mode-locked, pulsed Ti:Sapphire laser source
~70 ps time resolution
Frequency doubled for excitation
Single-photon avalanche diode detector
Fast electronics: arrival time measurements
Histogram of detected photons
Dye-Doped PFBT CPNs

## Slide 29: Picosecond Fluorescence Lifetimes of Dye-doped CPNs
Previous experiments indicate CPNs exhibit complex decay kinetics
  Stretched exponential lifetime decay
b is an indication of heterogeneity in exciton lifetimes
  Number varying between ~0.2 and 1
  As b decreases, indicates a broadening distribution of exciton lifetimes
  At b = 1, single exponential is recovered
Dye-Doped PFBT CPNs
Stretched Exponential
Exponential
Chen, R. J. Lumin. 2003, 102, 510-518

## Slide 30: Picosecond Fluorescence Lifetimes of Dye-doped CPNs
Mean exciton lifetimes reduced by doping (dynamic quenching)
  PFBT in THF fits well to single exponential (3 ns lifetime)
  CPNs fit best to bi-exponential and stretched exponential decays
  Decreasing trend in b as doping increases
  Dynamic self-quenching of perylene red emission at high doping ratios
Decreasing trend in b indicates a broadening distribution of exciton lifetimes as doping increases
  Agrees qualitatively with physical picture of exciton multiple energy transfer
  Range of exciton transfer distances broadens lifetime distribution
Dye-Doped PFBT CPNs
Groff, L. C., Wang, X., McNeill, J. D., J. Phys. Chem. C 2013, 117, 25748.

## Slide 31
Exciton Diffusion and FRET
Random Walk Model
Multichromophoric system--Frenkel Exciton
Excitons hop from site to site: hopping between polymer chains and segments, exciton transfers to dyes, quenchers or defects--Exciton diffusion
Hole polaron generation
emission/decay
Exciton transport modeled as a 3D random walk confined to a sphere
Results: excited state dynamics, quenching efficiency, blinking, twinkling
quencher
excitation
emission
diffusion path
Dye-Doped PFBT CPNs
C. Wu, J. McNeill et al., J. Phys. Chem. C, 2008, 112, 1772

## Slide 32
Exciton Diffusion Energy
Transfer Model for Dye-doped NPs
C. Wu, J. McNeill et al., J. Phys. Chem. C, 2008, 112, 1772
FRET rate
Radiative emission rate
Exciton diffusion
  Gaussian RNG
  Displacement per Dt
Average over many exciton trajectories and quencher positions
Results: Quenching efficiencies, Fluorescence decay kinetics
Dye-Doped PFBT CPNs

## Slide 33: Modeling of Dye-Doped PFBT Fluorescence
Average over many excitons, particles, quencher positions
  3000 excitons per particle, 50 particles per data point
  Poisson distribution of defects and quenchers
  Exciton diffusion length LD = 12 nm, Förster radius R0 = 4 nm
Approximate match to experimental TCSPC fitting results
  At 0% dopant, 2.3 defect quenchers (dye equivalents) present
  b reduced by implementing Poisson statistics
  Ignoring quenching by defects results in LD 2x lower, lower quality of agreement
Dye-Doped PFBT CPNs
Groff, L. C., Wang, X., McNeill, J. D., J. Phys. Chem. C 2013, 117, 25748.

## Slide 34: Dye-Doped PFBT CPNs: Summary
Successfully red-shifted emission via dye-doping
  High energy transfer efficiency and F at moderate doping
Nanoparticle samples exhibit complex decay kinetics
  Described best by bi-exponential or KWW dynamics
  Decreased lifetimes in doped samples (dynamic quenching)
  Acceptor is dynamically quenched at high doping ratios
Exciton diffusion, Energy Transfer Model matches experimental dynamics well
  Poisson distribution of defects and quenchers
  ~2 defects/CPN
  Length scale of exciton transport ~12 nm for PFBT (D = 8x10-9 m2 s-1)
C. Wu, J. McNeill et al., ACS Nano, 2008, 2, 2415
Dye-Doped PFBT CPNs

## Slide 35: Solvent-Induced Swelling of CPNs
Solvent-Induced Swelling
conjugated polymer nanoparticle
conjugated polymer film
conjugated polymer in solution
Use solvent-induced swelling methods to probe the changes in nanoparticle photophysics
  Probe rates of multiple energy transfer
  Determine nature of quenching defects (aggregates vs. oxidative)
Rate of exciton motion hypothesized to be amplified for CPNs
  Densely packed chromophores
  Access to more nearest neighbor chromophores in CPNs vs. polymer in solution
  Probe via fluorescence anisotropy decay (FAD) and modeling
Rapid mixing with
water, THF Removal
THF Addition

## Slide 36: Fluorescence Quantum Yield and Spectral Shifting
Increase in F as %THF increases
  ~92% quenching at 0% THF
  FTHF is recovered at high THF concentrations
Normalized spectra show progressive blue shifting of emission peak
  ~5 nm for PFBT
  ~40 nm for MEH-PPV
  Stronger dipole coupling in MEH-PPV
Solvent-Induced Swelling
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.
MEH-PPV
PFBT
PFBT
MEH-PPV

## Slide 37: Fluorescence Decay Kinetics of Swelled CPNs
Exciton lifetimes increase with increasing THF volume fraction
  PFBT in THF fits well to single exponential (3 ns lifetime)
  All others fit best to bi-exponential and stretched exponential decays
  b increases with increasing THF, except PFBT in 80% THF
Increasing trend in b indicates a narrowing distribution of exciton lifetimes as THF fraction increases
  Multiple energy transfer is FRET mediated (R-6 dependence)
  As CPN structure swells, neighboring chromophores become less accessible, reducing exciton mobility.
Solvent-Induced Swelling
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.
MEH-PPV
PFBT

## Slide 38: Fluorescence Decay Kinetics of Swelled CPNs
Evidence for possible dynamic equilibrium between CPNs and unassociated polymer
  Drastic decrease in b to ~0.2 at 80% THF for PFBT suggests sudden increase in lifetime distribution
  Bi-exponential fitting results
    PFBT Short time constant ~ CPN lifetime (~275 ps)
    PFBT Long time constant ~ polymer lifetime (~3 ns)
    Weighted amplitudes shift for higher THF concentrations
    Similar lifetime behavior for MEH-PPV between 40-60% THF.
Solvent-Induced Swelling
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.
MEH-PPV
PFBT

## Slide 39: Probing Energy Transport via Fluorescence Anisotropy Decay
Challenge: Indistinguishable chromophores
  Energetically degenerate, or near-degenerate
  TCSPC can measure kinetics
  Need method of measuring rate of energy transfer
Time-resolved fluorescence anisotropy decay
  Emission polarization is altered: rotational dynamics or energy transfer
  Typical uses: rotational diffusion of macromolecules, small molecules
Polarization changes due to energy homotransfer events
  (ns-µs), depending on particle size
  for 10 nm particle
  Rotational motion is negligible for CPNs
Solvent-Induced Swelling
Stokes-Einstein Equation
Fluorescence Anisotropy Decay
Equation
Cross, A. H., Fleming G. R., Biophys. J. 1984, 46, 45-56.
Beechem, J. M., Brand, L. Annu. Rev. Biochem. 1985, 54, 43-71

## Slide 40: Polarization Loss via Exciton Diffusion
Polarized excitation source
  CPNs possess randomly oriented transition dipoles
  Preferentially excite chromophore transition dipoles aligned relative to excitation
FRET to neighboring chromophore with imperfectly aligned transition dipole
  Each ET event alters polarization
  Emission polarization depends on T. dipole alignment prior to decay
  Measure intensity decays at 0°, 90°, 55° polarizations to construct ansiotropy decay
Fundamental Questions
  How many transfer events occur within the exciton lifetime?
  What is the length scale of these transfers?
Proposed Research
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.

## Slide 41: Picosecond Fluorescence Anisotropy Decay
Measure fluorescence polarization loss as a function of time
  Collect intensity decays at 0°, 90°, 55° polarizations relative to excitation source
  Rotational diffusion does not affect polarization loss
  Polarization loss due to multiple energy transfer of excitons
Intricate fitting analysis to extract anisotropy parameters
  Convolution fitting of polarized intensity decays
  Determine limiting anisotropy r0 and correlation time tc from fit results
  r0 gives information about transition dipole alignment at t0
  Able to measure rate constant ket from correlation time, tc
Solvent-Induced Swelling
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.
Cross, A. J., and Fleming, G. R., Biophys. J. 1984, 46, 45.

## Slide 42: Picosecond Fluorescence Anisotropy Decay
Multiple energy transfer rate constant amplified in CPNs
  For moderately swelled PFBT CPNs (above) ket ~3x1010 s-1
  For PFBT in THF, ket ~1x109 s-1
Hypothesized to be due to quantity of nearest neighbor chromophores to move between
  6 neighbors in CPNs, allow for motion along or between chains
  2 neighbors in linear polymer, motion is restricted along chain
Solvent-Induced Swelling
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.

## Slide 43: Discrete Lattice Modeling of Nanoparticle Swelling
Model Details
  Cubic lattice
  Energy transfer probability chromophore densities
  Initial lattice spacing determined from chromophore densities at ~1 nm
Defects/quenchers added to unswelled lattice until FCPN, tCPN reproduced
  Rq = 4 nm
  ~10 defects per CPN for both polymers
  Oxidized defects assumed (defects present regardless of chromophore density)
Quenching efficiency h defined via fluorescence quantum yield
Solvent-Induced Swelling
Multiple energy transfer probability
Defined from Random Walk
As lattice spacing increases,
pet reduced by f 4/3
Experimental quenching efficiency
Förster, T. Ann. Phys. 1948, 437, 55-75
Bardeen, C. J. Annu. Rev. Phys. Chem. 2014, 65, 127-148.
Groff, L. C., Jiang, Y., Wang X., and McNeill, J. D. 2015, in final preparation.

## Slide 44: Lattice Modeling Results
Model reproduces experimental h, t well
  For low to moderate %THF
  b reproduced well for PFBT
Model/experiment divergence at mid/high THF concentrations
  ascribed to dynamic equilibrum
  absence of nanoparticle dissociation in model
Energy transfer rate constants extracted from pet
  CPN ET rate constants 10-60x higher than polymer ET rate constants
  Agrees with experimental anisotropy fit results
  Agrees qualitatively with Förster exciton diffusion theory
    Reduced chromophore number density reduces ET rate
Solvent-Induced Swelling
Bardeen, C. J. Annu. Rev. Phys. Chem. 2014, 65, 127-148.
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.
MEH-PPV Model Results
PFBT Model Results

## Slide 45: Fluorescence Quantum Yield/Exciton Mobility Tradeoff
ket is ~2x higher for MEH-PPV CPNs compared to PFBT CPNs
  Due to stronger transition dipole coupling in MEH-PPV
F is ~4x higher for PFBT CPNs compared to MEH-PPV CPNs
  Weaker coupling/more isolated chromophores
Increased exciton motion efficiently funnels excitons to defect quenchers
  Reduction in lifetime
  Reduction in F
Solvent-Induced Swelling
Groff, L. C., Jiang, Y., Wang, X., and McNeill, J. D. 2015, In final preparation.

## Slide 46: Summary
Successfully prepared redshifted PFBT CPNs with high F
Determined LD ~12 nm for PFBT
Successfully used solvent-induced swelling to probe rates of exciton mobility using FAD
Multiple energy transfer amplified 10x-60x in CPNs versus polymer in solution
Lattice model results match well assuming oxidized defect quenchers
Tradeoff between mobility and F can be exploited for improvement of organic semiconductor devices

## Slide 47: Acknowledgments
Dr. Jason McNeill
McNeill Group
  Xiaoli Wang
  Yifei Jiang
NSF, NIH
Clemson University Department of Chemistry
You for your time and patience!
http://www.nsf.gov
http://www.nih.gov

## Slide 48
Backup slides

## Slide 49
Why are the particles nearly spherical?
Pi-conjugated backbone is rigid
Should yield oblong particles / rods
However...
Very hydrophobic: high polymer-water interface tension
Small particle size (High surface/volume ratio)
Favors nearly spherical shape
Confirmed by AFM, TEM, Preliminary Neutron Scattering

## Slide 50: Stern-Volmer Derivations
Static Dynamic

## Slide 51: Useful Equations
Quantum Yield Calc
Quantum Yield (Rates)
Absorption Cross-section

## Slide 52: Hole Polarons: Photogeneration and Luminescence Quenching
  Quasiparticle, radical cation and local polarization field
  caused by reversible photoejection of e-
  Hole polaron can diffuse between chromophores or recombine with electron
  Extremely efficient fluorescence quenchers
    One polaron quenches ~90% of fluorescence from a polymer chain of >100 chromophores
    Significant quenching at 5x1017 holes per cm3 of polymer (exceeded in devices)
e-
+
Background
Yu, J., Wu, C. F., Tian, Z. Y., and McNeill, J. D. Nano Lett. 2012, 12, 1300-1306
Yu, J., Song, N. W., McNeill, J. D., Barbara, P. F. Isr. J. Chem. 2004, 44, 127-132.